## Slide 1
Phase-field modeling and verification of multiphase transition processes at Tin-based electrode
Name： Qi Huang
E-mail： qihuang0908@163.com;
huang.qi@partner.kit.edu;
Supervisor： Prof. Dr. Yong Du, Prof. Dr. Britta Nestler

## Slide 2: 1. Previous work – nanoparticle
Background - electrode nanoparticle
high theoretical capacity
large volume deformation
multiphase transformation
, , ,
, ,
, and
(or )
Xinwei Zhou, ACS Applied Materials & Interfaces, 2019.

## Slide 3: 2. Current work – nanoparticle
Phase-field Modeling of polycrystalline nanoparticle
Cu-Li-Sn system, Fan Zhang, Journal of Alloys and Compounds, 2019

## Slide 4: 2. Current work – nanoparticle
intercalation + thermodynamic data
Reference states are bcc-Li, bct-Sn (Sn) and fcc-Cu.
Phases | calculated formation energy | Component ratio
 |  | 0.0, 0.5
 |  | 0.2, 0.4
 |  | 0.5, 0.25
 |  | 0.0, 0.7
 |  | 0.25, 0.5
Phases |  | Component ratio
 |  | 0.2, 0.4
 |  | 0.5, 0.25
 |  | 0.0, 0.7
 |  | 0.25, 0.5

## Slide 5: 2. Current work – nanoparticle
intercalation + thermodynamic data
Define
Define
A值的确认

## Slide 6: 2. Current work – nanoparticle
intercalation + thermodynamic data
Init multigrain structure (100 grains in nanoparticle, box = 128 x 128 x 128)

## Slide 7: 2. Current work – nanoparticle
intercalation + thermodynamic data
Relax interface

## Slide 8: 2. Current work – nanoparticle
intercalation + thermodynamic data
Merging phases

## Slide 9: 2. Current work – nanoparticle
intercalation + thermodynamic data
多晶电极颗粒，嵌锂过程

## Slide 10: 2. Current work – nanoparticle
intercalation + thermodynamic data + elastoplastic data
Phases | C11 | C22 | C33 | C44 | C55 | C66 | C12 | C13 | C23 | C15 | C25 | C35 | C46
 | 69.20 | 69.20 | 74.88 | 21.28 | 21.28 | 9.48 | 18.11 | 28.50 | 28.50 | - | - | - | -
 | 92.6 | 92.6 | 153.9 | 28.64 | 28.64 | 23.24 | 30.56 | 31.75 | 31.75 | - | - | - | -
 | 116 | 116 | 233 | 36 | 36 | 37 | 43 | 35 | 35 | - | - | - | -
 | 159 | 159 | 159 | 79 | 79 | 79 | 129 | 129 | 129 | - | - | - | -
 | 60.64 | 80.80 | 87.30 | 12.00 | 38.91 | 38.94 | 20.60 | 19.34 | -5.63 | -15.9 | 8.29 | 7.60 | 7.77
 | 69 | 69 | 69 | 52 | 52 | 52 | 43 | 43 | 43 | - | - | - | -
Phases | C11 | C22 | C33 | C44 | C55 | C66 | C12 | C13 | C23 | C15 | C25 | C35 | C46
 | 69.20 | 69.20 | 74.88 | 21.28 | 21.28 | 9.48 | 18.11 | 28.50 | 28.50 | - | - | - | -
 | 92.6 | 92.6 | 153.9 | 28.64 | 28.64 | 23.24 | 30.56 | 31.75 | 31.75 | - | - | - | -
 | 116 | 116 | 233 | 36 | 36 | 37 | 43 | 35 | 35 | - | - | - | -
 | 159 | 159 | 159 | 79 | 79 | 79 | 129 | 129 | 129 | - | - | - | -
 | 60.64 | 80.80 | 87.30 | 12.00 | 38.91 | 38.94 | 20.60 | 19.34 | -5.63 | -15.9 | 8.29 | 7.60 | 7.77
 | 69 | 69 | 69 | 52 | 52 | 52 | 43 | 43 | 43 | - | - | - | -
phases |  |  |  |  |  | 
Shear modulus | 18.49 | 31.75 | 45 | 53 | 25.55 | 36
phases |  |  |  |  |  | 
Shear modulus | 18.49 | 31.75 | 45 | 53 | 25.55 | 36

## Slide 11: 2. Current work – nanoparticle
intercalation + thermodynamic data + elastoplastic data
本征应变模型

## Slide 12: 2. Current work – nanoparticle
intercalation + thermodynamic data + elastoplastic data

## Slide 13: 2. Current work – nanoparticle
Results & Discussions 1: Verification
, ,
Define:

## Slide 14: 2. Current work – nanoparticle
Results & Discussions 2: Cu content

## Slide 15: 2. Current work – nanoparticle
Results & Discussions 3: Crack propagation

## Slide 16: 4. The End
Thanks for listening !

## Slide 17
Cu-Li-Sn system, Fan Zhang, Journal of Alloys and Compounds, 2019

## Slide 18
Cu-Li-Sn system, Fan Zhang, Journal of Alloys and Compounds, 2019